## Slide 1
（用于电路板的PCB铝板 ）
ALUMINIUM ENTRY MATERIAL
( PCB)
GUANGXI BAI SHENG LIGHT METAL MATERIAL CO., LTD
http://www.suncity-metal.com

## Slide 2
TOLERANCE：
GAUGE TOLERANCE: +0.01MM/-0
WIDTH TOLERANCE: +/-1MM
( OR AS AGREEMENT)
WIDTH TOLERANCE: +2MM,0MM
LENGTH TOLERANCE: ±1.5MM
MECHNICAL PROPERTY：
AS PER ASTM B 208. OR AGREEMENT
SURFACE:
UNIFORM AND BRIGHT SURFACE,CLEAN,FLATNESS FREE OF INCLUSIVE,SCRATCH,LINES,HOLES,ROLLING MARKS ETC DEFECTS WHICH INFULENCE MANUFACTURING OF OFFSET PLATE.
PACKING:SUITABLE LONG DISTANCE SEA TRANSPORTATION
COIL ID:
152MM/400MM/508MM.
SHEET:
ABOUT 1000PCS/BOX, INTERLEAVING PAPARE BETWEEN SHEETS
COIL:
STANDARD EXPORT EYE TO WALL OR EYE TO SKY PACKNING.
SPECIFICATION
FOR ALUMINIUM ENTRY MATERIAL ( PCB)
NOMINATION:
PCB IS USED FOR FURTHER PROCESSING FOR PRINTING
APPLICABLE FOR PRINTING
APPLICATION:
APPLICABLE FOR PRINTING
ALLOY AND SPECIFICATION( NORMAL):
ALLOY | TEMPER | SIZE(MM) | 
 |  | GAUGE(mm) | WIDTH(mm)
AA1100/1050 | H18/H16 | 0.15mm---0.17mm | 500mm---1350mm
 |  | 0.18---0.25mm | 700mm(W)*1350mm
GUANGXI BAI SHENG LIGHT METAL MATERIAL CO., LTD
http://www.suncity-metal.com

## Slide 3
2018/12/6
THE END
GUANGXI BAI SHENG LIGHT METAL MATERIAL CO., LTD
http://www.suncity-metal.com
广西佰晟轻金属材料有限公司